## Slide 2
(a) Reaction flow chart of CDE

## Slide 3
(b) Reaction flow chart of EDA Schiff base

## Slide 4
(c) Reaction flow chart of CY Schiff base

## Slide 5
Scheme 2. Flow chart of polyurethane synthesis

## Slide 6
(a)
(b)
Fig.1.(a) FTIR of CYS and CDE, (b) 1H-NMR spectra of CDE

## Slide 7
(a)
(b)
Figure 2.(a) FTIR of SAL、EDA and EDA Schiff base, (b) 1H-NMR spectra of EDA Schiff base

## Slide 8: Figure 3.(a) FTIR of CY and CY Schiff base, (b) 1H-NMR spectra of CY Schiff base
(a)
(b)

## Slide 9
(a)
(b)
Figure 4.(a) Raman spectra of CY, CY Schiff and CY-PU, (b) Total reflection infrared spectra of four polyurethanes BDO-PU, CYS-PU, EDA-PU and CY-PU, as well as a magnified image at the 1500 cm-1-1800 cm-1

## Slide 10
(a)
(b)
Fig.5.(a) The carbonyl peak-fitting profile of the CY-PU, (b) Degree of hydrogen bonding of different polyurethane samples

## Slide 11
(b)
(a)
Fig.6.TGA (a) and DSC (b) of polyurethanes with different chain extenders

## Slide 12
Figure 7. The damping factor curves for four polyurethane samples at 1 Hz (a), 10 Hz (b) and 50 Hz (c), respectively. (d) Master curve of CY-PU. (e) The translation factor of the CY-PU fits the curve. (f) Frequency extrapolation curve of CYS-PU, EDA-PU and CY-PU.

## Slide 13
Figure 8. Storage modulus of CY-PU, CYS-PU, BDO-PU and EDA-PU with 1 Hz (a), 10 Hz (b) and 50 Hz (c)

## Slide 14
Figure 9. Pictures of the scratch self-healing test of CYS-PU, EDA-PU and CY-PU. (a), (b) and (c) are at room temperature for 1 h. (a1), (b1) and (c1) are at 40 ℃ for 30 min. (a2), (b2) and (c2) are at 40 ℃ for 60 min.

## Slide 15
Figure 10.(a), (b) and (c) show the self-healing stress-strain curve of CY-PU, CYS-PU and EDA-PU, respectively. (d) is data on the self-healing properties of CY-PU, CYS-PU and EDA-PU.

## Slide 16
Figure 11. Self-healing mechanism of CY-PU